## Slide 1: deschutes county road department gravel road conversion pilot projects (otta seal and AC grindings) March 15, 2016 enhanced gravel road workshop

## Slide 2: Existing gravel road maintenance program
System Data:
  200 miles of gravel road
  Maintenance demand/service levels:
Activity/Data | High | Medium | Low
Grading frequency | 2 or 3 times per year | Annually or every other year | Infrequent/upon request
Dust palliative | Annual | None | None
Material add | 8+/- years | 12+/- years | >20 years
$/Mile/Year | $5,000/$7,500 | $2,500/$3,500 | <$1,500
# of miles +/- | 50 | 70 | 80
Local/Residential road annual surface maintenance (paved): $6,000/$8,000/mi/yr.

## Slide 3: Current Dust abatement program
Deschutes County has used Magnesium Chloride for 10-15 years.
Magnesium Chloride is hygroscopic. It draws and attracts moisture from the atmosphere to provide a wet looking surface and reduce airborne dust particles.
Deschutes County has experimented with other products.
Magnesium Chloride: The best dust palliative for roads in the high desert.
  Hygroscopic in low humidity
Added benefit of material stabilization.

## Slide 4: The problem: high maintenance gravel roads
1. Negative attributes of Magnesium Chloride dust palliative.
  Draws fines to surface which create slick and mucky conditions during freeze/thaw periods.
  Sticks to tires/wheels and tracks into driveway/garage.
  Can impact some roadside vegetation (Juniper kill).
2. Customer dissatisfaction with road condition and negative attributes:
  Leads to more service requests
  Higher costs
3. Rural gentrification
  City folk moving to the country
4. Other issues

## Slide 5: 18540 nw plainview road: $1.4M

## Slide 6: Road treated with Magnesium Chloride freeze/thaw

## Slide 7: Road treated with magnesium chloride tree kill

## Slide 8: Road treated with magnesium chloride potholing

## Slide 9: Typical gravel road washboarding

## Slide 10: The goal
Find an improved low-cost surface treatment with annual surface maintenance costs that are at or near that of a high maintenance gravel road ($5,000/$7,500/mi/yr.)
Target low-volume Local/Residential facilities.
Evaluate/estimate long-term maintenance costs and strategies.
Potentially develop/evaluate partnership opportunities with adjacent property owners (ie, a “maintenance LID”) to fund the upgrade.

## Slide 11: Pilot project treatments
Otta Seal
Developed in Norway in 1960s. Relatively new to USA.
Aggregate (1”-minus) rolled into a layer of high-float liquid asphalt.
Life Expectancy: 8-12 yrs.
A poor-man’s oil mat.
Paving with Asphalt Grindings
Asphalt grindings are milled from County roads prior to certain overlay projects.
Asphalt grindings are becoming more frequently used in a variety of maintenance applications.
  From “high-end gravel” replacement to reconstituted asphalt mix.
Life Expectancy: Varies

## Slide 12: Otta seal: research
Various webinars, conferences and seminars introduced concept.
Various publications: Minnesota DOT
Internet searches, etc.
Vendor experience with similar seals
  Bituminous surface treated (BST)

## Slide 13: Otta seal equipment
Asphalt Distributor
Chip Spreader
Pneumatic-tired roller
Steel roller
Broom
Water Truck

## Slide 14: Otta seal materials
Binder: High Float Medium Set Oil: HFMS-2
Aggregate: Gradation varies based on traffic loading
  Low quality, non-paving spec rock
  0.5” to 1” Max
  Up to 10% fines
  Dirty!
Again…..A Poor Mans Oil Mat

## Slide 15: Some gradation spec examples
International Focus Group
Washington vendor presentation
Dense = Higher than 100 ADT

## Slide 16: Deschutes county otta seal rock
Dense Specification: (19 mm = ¾” and 0.075mm = #200 sieve)

## Slide 17: Pilot project – otta Seal Plainview road
Plainview Road:
  East of Sisters (Fryrear Road)
  0.90 mile segment, 18’ – 20’ wide
  Local/Residential classification, dead end.
  Low ADT (110± vpd)
  Frequent calls for maintenance
    Dust complaints (residences are close to the road).
    Grading requests.
    Juniper tree kill.

## Slide 18: Pre-installation (typical of post grading)

## Slide 19: Pre-installation (note: dying roadside junipers)

## Slide 20: HFMS-2 Application (0.48-50 Gal/sy) (road pre-wet, 1-hour prior)

## Slide 21: Single pass with chip spreader (1”–minus “dirty” Material)

## Slide 22: Break of HFMS (Medium set)

## Slide 23: Immediate Post agg application ready to roll

## Slide 24: Otta seal installation

## Slide 25: Otta seal installation
Application recommendations = Roll, roll, roll, roll, roll
DC Experience: 8-hrs (on installation day)

## Slide 26: Otta seal installation post installation with sand seal – first week

## Slide 27: At 1-month

## Slide 28: Surface integrity (very dirty appearance)

## Slide 29: 7 months later…

## Slide 30: At 7 months: Some flaws

## Slide 31: Otta seal installation cost
Notes:
Personnel Rate Multiplier: 3.15 (fully loaded, with overhead)
Equipment rates include depreciation.
Hypothetical break-even point: 7.3 years

## Slide 32: Otta seal: lessons learned
Felt aggregate was “too dirty” and difficult to apply uniformly.
  Was it too dirty or could the chip spreader not “keep up”
  May use aggregate with fewer fines in future Otta seal.
Will not use 10-ton double-drum roller again.
  Too much vibe or weight promoted “sticking” to drums
  Lighter rollers preferred.
Segregation in chip spreader – especially in center.
  Will seal one lane at a time to narrow width of spread.
  Fewer fines will help alleviate some segregation – maybe?
Deschutes County has 2.0 miles of Otta Seal planned in 2016 (fall)

## Slide 33: Next steps – otta seal
1. Evaluation of Treatments
  Monitor initial degradation and estimate near-term and long-term maintenance needs.
    Is this a product we can chip seal and roll into our Pavement Management Program?
      If so, at what interval for first chip seal and what is the subsequent frequency of treatments?
      If not, what alternative maintenance treatments or strategies are necessary?
2. Cost Analysis
  How do the initial and projected maintenance investment levels compare to the annual average maintenance investment for gravel roads?
3. Refine the Process
  What refinements can we make to our application technique to reduce the initial application cost of the Pilot Projects?

## Slide 34: Pilot project – AC Grindings Ivancovich Way
Ivancovich Way:
  Northeast of Redmond
  Local/Residential classification, dead end.
  0.60 mile, 24’ wide
  Low ADT (150± vpd)
  Frequent calls for maintenance
    Grading requests to address washboarding.
    Tracking of muck layer during freeze/thaw and wet periods.

## Slide 35: Ac grinding Project
Goal: Low-cost application of grindings – could apply hot mix for $9-$12/SY
Age of grindings: 2-years
Re-ground to 1/2”
2 – 2” lifts
Added water prior to compaction
Experimented with adding diluted tack mid-compaction

## Slide 36: AC Grindings installation pre-installation

## Slide 37: Ac grindings installation 2-2” lifts

## Slide 38: Ac grindings installation water/tack with compaction

## Slide 39: Ac grindings installation

## Slide 40: Ac grindings installation sand seal finish

## Slide 41: At 7 months

## Slide 42: At 7 months – some flaws

## Slide 43: Lessons Learned
Heat is your friend.
  Very concerned during morning period - feared project failure.
  Afternoon heat allowed material to bind – saved the project.
Be mindful of over-compaction during initial roll – especially vibratory.
Ease into the rolling effort.
Rock shoulders quickly – edges can be soft and need support.
Early to mid-Summer installation (heat) versus late Summer.
Community education to drive slow during first month +/-; curing period.

## Slide 44: AC Grindings installation cost
Notes:
Personnel Rate Multiplier: 3.15 (fully loaded, with overhead)
Equipment rates include depreciation.
Hypothetical break-even point: 10.6 years