## Slide 1: UTILIZING GRINDINGS ON RURAL ROADS:
Converting Gravel Roads to Hard Surface

## Slide 2
Smith Loop Before Grindings Application
2 miles of gravel road
Approximately 4 inches of gravel
Daily traffic count of 100

## Slide 3: Bad Grinding Source
Quality of Product Source Very Important
Be wary of
Large alligators
F mix road
Road that has fabric

## Slide 4: Good Grinding Source
Quality of the surface that is being torn up will affect the size of the resulting product.
Look for
Smooth surface
Not a lot of patching
No fabric
Will result in consistent product

## Slide 5: Manage Production Rates
Know your source’s production rate,
Know your production rate,
Make a plan to control both.
e.g. We designate a stockpile site where loads can be staged.
To control the quality of work:

## Slide 6: Water is Very Important in the Process: Have a Consistent Source
Helps product bind together
Helps control
fines: brings
them to surface
Source should be close
It will take more than you think

## Slide 7: Phase 1: First Grader
First pass
Works larger grindings toward the center of the road
Sets depth of grindings
Levels surface
Lays out bigger grindings for roller

## Slide 8: Larger Grindings Pulled to the Middle of Road

## Slide 9: Elliott Grid Roller Breaks larger pieces to finished size
Breaks down grindings more consistently than a sheep foot roller
2) Doesn’t leave
holes in road
surface

## Slide 10: Second Grader with a Roller
First grader determines depth
Second grader shapes road
Smooth Roller follows and compacts to grade

## Slide 11: Grindings are also used to Build up Intersections and Approaches

## Slide 12: Phase 2: Chip Seal Process
After final roll, no traffic is allowed on the road until the first lift of chip seal is done.

## Slide 13: Double Chip Seal
Two options:
Two lifts of 3/8” rock (better for high truck traffic)
OR
    One lift of 3/8”, and 1 of ¼” (better for bikes)
Shot rate: .40

## Slide 14: Phase 3: Fog Seal
Final step is the application of a fog seal:
Better seal Binding effect

## Slide 15: Finished Product
20 Foot Road Surface

## Slide 16: Six years later
Tight surface
Dime

## Slide 17: Current Photo
No Base Failures

## Slide 18: Cost Summary
Base Cost:
Material
Grindings $10.20/ton for 4044tons $41,251.00
Equipment
County $11,043.00
Rental $12,400
Labor
County $17,870
Total Base Cost: $82,564.00
Surface Cost:
Chip Seal $60,000.00
Fog Seal $2,400.00
Total Surface Cost: $62,400.00
Total Cost: $144,964.00
Roughly $72,482 per mile

## Slide 19
Tampico After One Year
Traffic count on this road is 250/day

## Slide 20: Tampico with 3/8 and ¼ Chip Seal

## Slide 21
Any Questions?