## Slide 1: Engineered Emulsion for tack/bond coat and fog/mastic seal
Troy Tindall
Blue Line transportation / Enviroad llc

## Slide 2: Engineered Emulsions
Engineered emulsions are designed to address performance challenges faced when utilizing specification emulsions.
  Tracking
  De-bonding
  HMA compaction
  Loss of coating
  Loss of skid resistance

## Slide 3: Specification Tack Coat
Specification tack coats are asphalt emulsions that conform to a wide specification range and have been the the industry standard over many years.

## Slide 4: Specification CSS-1H
CSS-1H | Test Method | Specification | 
Tests on Emulsion: |  |  | 
 |  | MIN MAX | 
Saybolt Viscosity @ 250C (770F), SFS | AASHTO T 59 | 20 | 100
Storage Stability1, % (1 day) | AASHTO T 59 | - | 1.0
Sieve Test, % | AASHTO T 59 | - | 0.10
Cement Mixing Test, % | AASHTO T 59 | - | 2.0
Particle Charge Test | AASHTO T 59 | Positive | -
Distillation2 to 2600C (5000F) Oil distillate % (by volume of emulsion) | AASHTO T 59 | - | 3.0
Residue, % (by weight) | AASHTO T 59 | 57.0 | -
Tests on Residue by Distillation: |  |  | 
Penetration @ 250C, (770F), 100g, 5s dmm | AASHTO T 49 | 40 | 90
Ductility @ 250C, (770F), 5.0cm/min, cm | AASHTO T 51 | 40 | -
Solubility in TCE, % | AASHTO T 44 | 97.5 | -

## Slide 5: CSS-1H - Tracking

## Slide 6: CSS-1H - Tracking

## Slide 7: CSS-1H - Tracking

## Slide 8: CSS-1H - Tracking

## Slide 9: CSS-1H - De-bonding in wheel path

## Slide 10: CSS-1H - De-bonding in wheel path

## Slide 11: CSS-1H - HMA creep during compaction

## Slide 12: ODOT High-Performance Tack Coats (HPTC)
In 2015 Oregon Department of Transportation initiated the HPTC study. Working in conjunction with Oregon State University and interested asphalt suppliers, ODOT challenged the idea that engineered emulsions could provide the bond coat that just couldn’t be attained with specification tack coats.
  No specification – bring your game
  In-field laboratory controls
  Consistent application and testing equipment
  Laboratory testing of emulsions and bonding characteristics

## Slide 13: HPTC

## Slide 14: HPTC

## Slide 15: HPTC

## Slide 16: HPTC

## Slide 17: HPTC

## Slide 18: HPTC

## Slide 19: HPTC

## Slide 20: HPTC

## Slide 21: Engineered Bond Coat
Engineered bond coats address the primary issues faced when using specification tack coats by ensuring the bond is maintained during paving operations. Eliminating tracking insures the desired bond between layers is achieved and promotes compaction through reduction of mix creep.
  Project type – overlay or mill & fill
  Temperatures - Day or night paving
  Traffic requirements
  Storage requirements

## Slide 22: EARTHBIND® NTBC-41 NON-TRACK BOND COAT
 | Test Method | Specification | 
Tests on Emulsion |  |  | 
 |  | MIN MAX | 
Saybolt Viscosity @ 250C (770F), SFS | ASTM D7496 | 10 | 75
Sieve Test, % | ASTM D6933 | - | 0.1
Residue, % by Evaporation (weight) | ASTM D6934 | 10 | -

## Slide 23: EARTHBIND® NTBC-41

## Slide 24: EARTHBIND® NTBC-41

## Slide 25: EARTHBIND® NTBC-41

## Slide 26: EARTHBIND® NTBC-41

## Slide 27: EARTHBIND® NTBC-41

## Slide 28: EARTHBIND® NTBC-41

## Slide 29: EARTHBIND® NTBC-41

## Slide 30: EARTHBIND® NTBC-41

## Slide 31: EARTHBIND® NTBC-41

## Slide 32: EARTHBIND® NTBC-41

## Slide 33: Specification Fog Seal
Specification fog seals are asphalt emulsions that conform to a wide specification range and have been the the industry standard over many years.

## Slide 34: CSS-1 Dilute

## Slide 35: CRS-2P / HFRS-P1 Dilute

## Slide 36: Engineered Fog / Mastic Seal
Engineered fog / mastic seals are formulated to meet customer expectations utilizing project data.
  Average daily traffic
  Type of traffic
  Environmental / Time of day considerations
  Road condition
  Skid resistance
  Return to traffic requirements

## Slide 37: BL-Fog

## Slide 38: BL-Fog

## Slide 39: BL-Fog

## Slide 40: BL-Fog

## Slide 41: BL-Fog

## Slide 42: BL-Fog

## Slide 43: BL-Microcoat

## Slide 44: BL-Microcoat

## Slide 45: BL-Microcoat

## Slide 46: BL-Microcoat

## Slide 47: BL-Microcoat

## Slide 48: BL-Microcoat

## Slide 49: BL-Microcoat

## Slide 50: BL-Microcoat

## Slide 51: BL-Microcoat

## Slide 52: Questions?
Troy Tindall
Blue Line Transportation / Enviroad LLC
troy@bluelinetrans.com
503-702-1236