## Slide 1: SAMI
Stress Absorbing Membrane Interlayer

## Slide 2: 2017 Helmick Rd Overlay
Todd Whitaker, PE
Polk County Public Works

## Slide 3: History
Original Construction – 1928
- Cummins & LaPointe
Widening – 2007
- Knife River
North Overlay – 2012
- North Santiam Paving
- Level 3, ½” HMAC, 2” thickness
- w/o Crack Control
South Overlay – 2017
- Salem R&D
- Level 2, ½” HMAC, 3” thickness
- With Crack Control

## Slide 4: 2017 Overlay
Total Length = 4 miles
Crack Control Methods
Method 1 – Double Chip Seal
Method 2 – Paving Grid

## Slide 6: Double Chip Seal
Emulsion – Blue-Line CRS-3P @ 0.42 gal/SY
1st Layer:
Oil Shot – 0.42 gal/sy
Aggregate – 3/8”-#4 @ 26 lbs/SY
As-Built shows 20 lbs/SY
2nd Layer (1 week later):
Oil Shot – 0.42 gal/SY
Aggregate 3/8”-#4 @ 26 lbs
Cost: $4/SY
Total Area of treatment: 55,000 SY

## Slide 7: Composite Paving Grid
- Mirafi PGM-G4
Cost: $7/SY installed
Total area of treatment: 750 SY total

## Slide 8: Results and Conclusions
5 years later
- No observed cracking in southern section
- No difference between double chip and geogrid performance (yet)
- Polk County will continue monitoring
- Double chip seal shows promise as a crack control treatment

## Slide 9: SAMI
Marion County
Arndt Road NE
OACES Chipseal Workshop
March 21-22, 2023
Hood River OR

## Slide 10: Arndt RD NE -SAMI Treatment
OACES Chipseal Workshop
March 21-22, 2023
Hood River OR
1.3-mile segment located in northern Marion County. Completed July 2022
Collector in the northern region that connects Aurora area to St Paul Hwy with ADTs of 1,892
High maintenance section with regular pothole repairs and patching with a PCI of 14.
Pavement design recommended full depth reconstruction and a 6” HMA overlay.
Urgent need to repair due to increased traffic from the current ODOT I-5 Aurora/Donald Interchange Project.

## Slide 11
OACES Chipseal Workshop
March 21-22, 2023
Hood River OR
Preliminary prep work involved filling in potholes and delaminated areas

## Slide 12
OACES Chipseal Workshop
March 21-22, 2023
Hood River OR
Applied levelling courses over the patches

## Slide 13
Single shot scrub seal (Sierra Santa Fe) using a polymer modified rejuvenating emulsion (PMRE)
Shot rate = ~.38 gal/sq yd.
OACES Chipseal Workshop
March 21-22, 2023
Hood River OR

## Slide 14
OACES Chipseal Workshop
March 21-22, 2023
Hood River OR
Applied a single layer of 3/8”- #4 chip over the scrub seal
@ ~ 25 lbs/sq yd

## Slide 15
Followed up with two lifts of 1” & 2” AC overlay.
QUESTIONS?
OACES Chipseal Workshop
March 21-22, 2023
Hood River OR

## Slide 16: SAMI
Five Rivers Road Overlay Project
10.5 mile long project; $4.5 million
Located in Lincoln County; 25 miles east of Waldport
Managed by theFederal Highway Administration
Contract awarded to Brix Paving Northwest, Inc.
Diamond Grind existing HMAC road surface for profile and crack seal material removal.
Scrub seal performed by Sierra Santa Fe as subcontractor.
Two inch asphalt concrete overlay placed by prime contractor.
Stress Absorbing Membrane Interlayer