## Slide 1
Road base stabilization
Pilot project: City Fleet parking lot, City of Portland

## Slide 2
City Fleet parking lot project
City Fleet’s parking lot donated to Legacy Emanuel hospital
ODOT leased parking lot selected as replacement
  Existing pavement heavily alligatored
  City Fleet  PBOT for cost effective solution
~2 month window for completion, August through September 2014

## Slide 3
Planning phase
Options considered:
  Reconstruction  $$$$$
  Epoxy existing surface  $$$$
  Full depth reclamation (FDR) with:
    Large aggregate chip seal  $$
    Thin lift (1.5”) asphalt  $$
Selected FDR w/thin lift asphalt
  Cost effective
  PBOT can pave
  Chip seal more sensitive to fall weather

## Slide 4
Pilot project goals
Try different soil stabilization techniques and products
Utilize different base sealing products
Employ new thin lift asphalt designs
Go fast – only 2 month window
Result: Lower initial/life cycle costs

## Slide 5
Pilot project elements
Soil stabilization strategies employed:
  Asphalt Zipper with Permazyme
  Pulverize with cement treated base
Base sealing products used:
  Enviroad - Earthbind 100
  Zydex Industries - Zycosoil
Thin lift asphalt paving mix design
  Cold climate asphalt: 58-28
  Richer mix (~6.0% oil content)
  ½” mix design at 1.5” depth
  Utilize long (1.25”) ACE Kevlar fibers

## Slide 6
Soil stabilization method 1:
Asphalt Zipper w/Permazyme
Permazyme

## Slide 7
Soil stabilization method 1:
Asphalt Zipper w/Permazyme

## Slide 8
Soil stabilization method 1:
Asphalt Zipper w/Permazyme

## Slide 9
Base sealing method 1:
Enviroad – Earthbind 100

## Slide 10
Soil stabilization method 2:
Pulverize w/cement treated base

## Slide 12
Soil stabilization method 2:
Pulverize w/cement treated base

## Slide 13
Base sealing method 2:
Zydex Industries - Zycosoil

## Slide 14
Cold climate asphalt: 58-28
Richer mix (~6.0% oil content)
½” mix design at 1.5” depth
Utilize long (1.25”) ACE Kevlar fibers
Thin lift asphalt mix

## Slide 15
Thin lift asphalt mix

## Slide 16
Thin lift asphalt mix

## Slide 17
Thin lift asphalt mix

## Slide 18
Thin lift asphalt mix

## Slide 19
58-28 mix design with ACE Kevlar fibers, at 1.5” depth over treated base holding up very well!
2 winter seasons - no cracks, raveling, delamination, or base failures
Project cost savings:
  Standard reconstruction = $200K+ (est)
  Pilot project cost = $88K
Pilot project summary

## Slide 20
Need clay content for enzymes to work; perform hydrometer test if unsure!
58-28 asphalt surprisingly effective
Pulverizing + soil stabilizer a fast, cost effective way to rehab streets in poor condition (i.e. beyond potholing)
Methods/products could be used to rehab low volume urban streets in poor condition
Use thin lift or chip seal over treated base
Lessons learned, going forward

## Slide 21
Residential street application?

## Slide 22
Questions